SUPPLEMENTARY MATERIAL:

In the following figures we present MEV images and chemical element analysis for the fossils A, B, C and D belonging to Pedra do Fogo Formation. As established in the paper, the sample A corresponds to the fossil of a gymnosperm, collected from Duque Bacelar municipality; the sample B corresponds to a pteridophyta fossil, also collected from Duque Bacelar; the sample C belongs to a gymnosperm fossil from Teresina municipality and the samples D, originated from Monsenhor Gil municipality, corresponds to a pteridophyta fossil specimen.

|  | Element Weight % Weight % σ Atomic % Aluminum 0.642 0.121 0.507 Silicon 39.328 0.404 29.880 Chromium 2.447 0.252 1.004 Iron 8.611 0.439 3.290 Oxygen 48.973 0.447 65.318 |
| --- | --- |

Figure S1 - Image obtained through MEV on the surface of sample A.

|  | Element Weight % Weight % σ Atomic % Aluminum 1.080 0.131 0.802 Silicon 45.791 0.341 32.665 Oxygen 53.129 0.343 66.533 |
| --- | --- |

Figure S2 - Image obtained through MEV on the surface of sample A.

|  | Element Weight % Weight % σ Atomic % Carbon 14.951 0.711 20.776 Aluminum 0.321 0.059 0.198 Silicon 20.853 0.365 12.392 Oxygen 63.874 0.716 66.634 |
| --- | --- |

Figure S3 - Image obtained through MEV on the surface of sample A.

|  | Elemente Weight % σ Atomic % Aluminum 4.736 0.509 3.682 Silicon 37.960 1.019 28.349 Iron 7.652 1.109 2.874 Oxygen 49.652 1.124 65.095 |
| --- | --- |

Figure S4 - Image obtained through MEV on the surface of sample B.

|  | Element Weight % Weight % σ Atomic % Aluminum 5.552 0.251 4.252 Silicon 38.706 0.488 28.473 Potassium 0.952 0.180 0.503 Iron 4.320 0.457 1.598 Oxygen 50.468 0.530 65.174 |
| --- | --- |

Figure S5 - Image obtained through MEV on the surface of sample B.

|  | Element Weight % Weight % σ Atomic % Carbon 12.627 2.443 18.048 Aluminum 0.318 0.065 0.202 Silicon 24.568 1.293 15.017 Potassium 0.275 0.063 0.121 Oxygen 61.969 2.394 66.494 |
| --- | --- |

Figure S6 - Image obtained through MEV on the surface of sample C.

|  | Element Weight % Weight % σ Atomic % Sodium 0.562 0.148 0.491 Aluminum 0.592 0.119 0.441 Silicon 45.503 0.354 32.554 Potassium 0.647 0.133 0.333 Oxygen 52.696 0.360 66.181 |
| --- | --- |

Figure S7 - Image obtained through MEV on the surface of sample C.

|  | Element Weight % Weight % σ Atomic % Aluminum 5.831 0.259 5.468 Silicon 19.710 0.398 17.757 Potassium 0.692 0.151 0.448 Iron 35.743 0.665 16.194 Oxygen 38.023 0.588 60.133 |
| --- | --- |

Figure S8 - Image obtained through MEV on the surface of sample D.

|  | Element Weight % Weight % σ Atomic % Carbon 5.941 2.843 9.492 Magnesium 0.558 0.121 0.441 Aluminum 7.349 0.471 5.227 Silicon 26.028 1.532 17.785 Potassium 0.929 0.134 0.456 Iron 5.147 0.458 1.769 Oxygen 54.048 2.806 64.831 |
| --- | --- |

Figure S9 - Image obtained through MEV on the surface of sample D.