

Image Name: NiS2#1952-1\_HP2

Image Resolution: 1024 by 768

Image Pixel Size: 1.29 µm

Acc. Voltage: 15.0 kV

Magnification: 100



Weight %

|  |  |  |
| --- | --- | --- |
|  |  ***S*** |  ***Ni*** |
| ***Amostra3b(2)\_pt1*** |  51.53 |  48.47 |

Atom %

|  |  |  |
| --- | --- | --- |
|  |  ***S*** |  ***Ni*** |
| ***Amostra3b(2)\_pt1*** |  66.07 |  33.93 |