


Image Name: NiS2#1952-1\_HP2

Image Resolution: 1024 by 768

Image Pixel Size: 1.07 µm

Acc. Voltage: 15.0 kV

Magnification: 119



Weight %

|  |  |  |
| --- | --- | --- |
|  | ***S*** | ***Ni*** |
| ***Amostra3b(1)\_pt1*** | 52.86 | 47.14 |

Atom %

|  |  |  |
| --- | --- | --- |
|  | ***S*** | ***Ni*** |
| ***Amostra3b(1)\_pt1*** | 67.25 | 32.75 |