


Image Name: NiS2#1952-1\_HP2

Image Resolution: 1024 by 768

Image Pixel Size: 1.61 µm

Acc. Voltage: 15.0 kV

Magnification: 80



Weight %

|  |  |  |
| --- | --- | --- |
|  | ***S*** | ***Ni*** |
| ***Amostra2b(3)\_pt1*** | 51.62 | 48.38 |

Atom %

|  |  |  |
| --- | --- | --- |
|  | ***S*** | ***Ni*** |
| ***Amostra2b(3)\_pt1*** | 66.15 | 33.85 |