


Image Name: NiS2#1928-2\_HP2

Image Resolution: 1024 by 768

Image Pixel Size: 1.98 µm

Acc. Voltage: 15.0 kV

Magnification: 65



Weight %

|  |  |  |
| --- | --- | --- |
|  | ***S*** | ***Ni*** |
| ***Amostra2b(2)\_pt1*** | 52.56 | 47.44 |

Atom %

|  |  |  |
| --- | --- | --- |
|  | ***S*** | ***Ni*** |
| ***Amostra2b(2)\_pt1*** | 66.98 | 33.02 |